## Slide 1
Physicochemical Study of Visible Light Photooxidation of Benzyl Alcohols using Metal-Organic Frameworks
Michelle A. Hettinger
Dr. Fernando Uribe-Romo
Undergraduate Research
Spring 2015

## Slide 2: Physicochemical Study of Visible Light Photooxidation of Benzyl Alcohols using Metal-Organic Frameworks
Introduction
  Photoredox catalysis
    Homogeneous
    Heterogeneous
    Metal-Organic Frameworks
  Objectives
    Develop a model
    Kinetics, Quantum Yield, Mechanism
Results
  Rates of reaction
  Photochemical Quantum Yields
  Future Work
Notes: Thank you, Dr. Kujawa. First I will talk about photoredox catalysis, both homogenous and heterogeneous, and show how MOFs impart the desirable properties of both types of catalysts. Then I will introduce the model I have developed for investigating the physicochemical properties of MOFs, like chemical kinetics, photochemical quantum yield, and probing the mechanism. Then I will show how the results that obtained which are the rates of reaction and photochemical quantum yield. And finally I will propose future research.

## Slide 3: Photoredox catalysis
Homogeneous (HOMO-LUMO excitation)
  Molecular catalyst: Ru(bipy)32+
    Soluble
Heterogeneous (generation of e-/hole pair)
  Solid-state catalyst: TiO2
    Insoluble
Notes: What is photoredox catalysis? When light is absorbed by the catalyst, the catalyst will enter a light-induced charge separated state which is redox active. The light activated redox catalyst can then oxidize or reduce organic molecules. Homogeneous catalysis involves a HOMO-LUMO excitation. The molecular catalyst tris(bipyridine)ruthenium(II) is a famous example of a soluble homogeneous photoredox catalyst. Heterogeneous catalysis involves the generation of an electron hole pair. Titanium dioxide is a good example of an insoluble solid state photoredox catalyst.

## Slide 4: Homogeneous Catalysis
Prier, C. K. et al. Chem. Rev. 2013, 113, 5322-5363.
Disadvantages
  Not reusable
  Purification of product
  Ru and Ir are expensive noble metals
Advantages
  Tunable for a wide range of reactions
  High selectivity with low potential for side reactions
  Employed in low loadings
Notes: I would like to further discuss the tris(bypiridine)ruthenium(II) complex. When visible light, at about 450 nm, is absorbed by the complex an electron from one of the metal centered t2g orbitals is excited to a ligand-centered pi star orbital. This transition is called a metal to ligand charge transfer and results in the ruthenium being oxidized to ru(III) and the ligand framework a single-electron reduction. The singlet state undergoes rapid intersystem crossing to give the lowest-energy triplet state, which has a long lifetime of about 1100 ns. In this triplet state the complex can act as either a reductant or an oxidant. When acting as a reductant the ligand framework donates an electron. When acting as a oxidant the t2g orbital of the metal center accepts an electron and ruthenium is reduced back to Ru(II). The advantages of such homogeneous catalysts is that the ligands can be tuned for a wide range of reactions to enhance selectivity. They can also be employed in low loadings. On the downside, however, they aren’t reusable and purification of product isn’t particularly simple. Also ruthenium and iridium (which can also complex with bipyridine) are expensive noble metals.

## Slide 5: Heterogeneous Catalysis
Mainly TiO2
  Evolution of H2 and O2 from H2O
  Reduction of CO2 with H2O to form hydrocarbons
  Decomposition of harmful organic compounds (eg. benzene)
Schneider, J. et al. Chem. Rev. 2014, 114, 9919-9986.
Disadvantages
  Large band gap
  Non-selective
  Lack tunability
Advantages
  Stability
  Reusability
  Reactivity
Notes: Next I would like to talk more about titanium dioxide as a photoredox catalyst. When light with enough energy to overcome the band gap strikes the catalyst an electron is excited into the conduction band an a hole is generated in the valence band. This electron/hole pair is then able to either reduce or oxidize organic molecules. Titanium dioxide is an extensively studied heterogeneous catalyst that is used in the evolution of hydrogen, reduction of carbon dioxide and decomposition of harmful organic compounds such as benzene. The advantages are its chemical stability against harsh conditions, thermally stable across a wide range of temperatures and reusability. On the downside it has a large band gap and inability to be fine tuned for specific reactions.

## Slide 6: Metal-Organic Frameworks
Characteristics
  Crystalline
  Highly porous
  Metal oxide clusters connected by organic linkers
Chen, T.-H. et al. Chem. Mater. 2014, 26, 4322-4325.
Advantages
  Highly tunable
  Solid
  Reusable
  Chemical/thermal stability
Notes: Now I would like to discuss metal organic frameworks and explain how they impart the desirable properties of the solid state and molecular catalysts I just talked about. MOFs are crystalline highly porous materials consisting of metal oxide clusters connected by organic linkers. These organic linkers can be modified in ways that can increase pore size or even to absorb more light. They have a high degree of chemical and thermal stability and since they are solids can be reused.

## Slide 7: Objectives of My Research
Develop a model for understanding the photoredox capabilities of MOFs
Task 1
  Prepare MOFs that can do photoredox catalysis
Task 2
  Set up experimental protocol for visible light photooxidation of benzyl alcohol
Task 3
  Investigate photochemical characteristics
    Kinetics
    Photochemical quantum yield
    Temperature dependence
    Mechanism
Notes: This brings me to the objectives of my research, which are to develop a model for understanding the photoredox capabilities of MOFs. I did this in three phases, or tasks. The first task was to find and prepare MOFs that can do photoredox catalysis. Then to set up an experimental protocol for the visible light photooxidation of my chosen substrate, aromatic benzyl alcohols. And finally to investigate the photochemical characteristics, such as the kinetics, photochemical quandum yield, temperature dependence and probing the mechanism.

## Slide 8: Task 1. Prepare MOFs
Chosen MOFs contain inexpensive transition metals
(V) MIL-47-NH2
(Ti) MIL-125-NH2
(Zr) UiO-66-NH2
Nasalevich, M. A. et al. Chemical Communications 2013, 49, 10575-10577.
vs.
Notes: The MOFs I chose contain inexpensive transition metals making use of the 2-aminoterephthalic acid linker. They are the vanadium based mil-47 amino, titanium mil-125 amino and zirconium uio-66-nh2. I would like to point out how the amino functional group red shifts the wavelength of maximum absorption more towards the visible region when incorporated into a MOF. So that is why we chose the amino version of the MOFs to do visible light photocatalysis.

## Slide 9: MOF Synthesis
Reaction mixture is placed in pyrex tube and frozen in liquid nitrogen. Pressure is reduced to 150 mtorr
Pyrex tube is flame sealed, brought to room temp. and placed in oven at 150 °C for 1-4 days.
Notes: So how is a MOF actually made? The reaction mixture is placed in a pyrex tube and frozen in liquid nitrogen. While frozen the pressure is reduced with a schlenk line to 150 mtorr and flame sealed with a torch to maintain that pressure. Then the pyrex tube is placed in an oven at 150 degrees celcius for one to four days after which it is filtered and washed with chloroform.

## Slide 10: Synthesis of MIL-47-NH2
Barthelet, K. et al. Angew. Chem. Int. Ed. 2002, 41 (2), 281-284.
Notes: I synthesized mil-47 amino by adding the linker with vanadium chloride in water. Here is the crystal structure. You can see the vanadium oxide cluster here and the linker that connects them. This MOF contains a one dimensional pore going into the plane of the board. And here is the powder xray diffraction as you can see matches with literature results.

## Slide 11: Optimization of MIL-47-NH2
TEA
Literature Synthesis
  1:1 Metal to Linker
  0.58 M VCl3
  15% Yield
  Poor reproducibility
My Synthesis
  1:0.25 Metal to Linker
  0.18 M VCl3
  2 drops of triethylamine
  60% Yield
  Better reproducibility
Reproducibility was enhanced with 2 drops of trimethylamine
Notes: Originally when I tried making this MOF I was getting poor yields and sometimes no product at all. So I optimized the synthesis and found that if I reduced the metal to linker ratio and concentration as well as adding 2 drops of trimethylamine I was able to obtain a 4 fold increase in my yield with better reproducibility. We think that a very small amount of triethyl amine helps to deprotonate the two carboxylic acids on the linker and thus facilitates in the formation of the MOF.

## Slide 12: Synthesis of MIL-125-NH2
Dan-Hardi, M. et al. J. Am. Chem Soc. 2009, 131, 10857-10859.
Notes: MIL-125amin was prepared by reacting the linker in titanium isopropoxide in a 9:1 mixture of DMF to methanol for one day. Here you can see the titanium oxide cluster that is connected by the linker to the other clusters. I obtained the PXRD and as you can see all the peaks correlate to that of the simulated data i obtained from materials studio.

## Slide 13: Synthesis of UiO-66-NH2
Cavka, J. H. et al. J. Am. Chem Soc. 2008, 130, 13850-13851.
Notes: The last MOF, UiO 66 amino was prepared by adding the linker with zirconium chloride in dmf for 1 day. You can see the cluster here and the linker here. I did powder xray diffraction and matched the bragg peaks with that of the simulated pattern.

## Slide 14: Objectives of My Research
Develop a model for understanding the photoredox capabilities of MOFs
Task 1
  Prepare MOFs that can do photoredox catalysis
Task 2
  Set up experimental protocol for visible light photooxidation of benzyl alcohol
Task 3
  Investigate photochemical characteristics
    Kinetics
    Photochemical quantum yield
    Temperature dependence
    Mechanism
Notes: So now that the first task was completed I could go on to the second task, to set up an experimental protocol for the visible light photooxidation of my substrate.

## Slide 15: Model Reaction
Cibulka, R. et al. Chem. Eur. J. 2004, 10, 6223-6231.
Oxidation of benzyl alcohols
R = H, OCH3, Cl, NH2
Alcohols to aldehydes
  Various industry applications
  Model for developing efficient and environmentally sound catalysts
Notes: The model reaction I chose was the oxidation of benzyl alcohol into benzaldehyde. In principle I could test various substituents, but I chose methoxy for simplicity sake. The alcohol to aldehyde has various industrial applications and this group led by cibulka et al found that it served as a good model for developing new catalysts.

## Slide 16: Visible light photooxidation
Specifically photooxidation of p-methoxybenzyl alcohol
MOF = MIL-47-NH2
MIL-125-NH2
UiO-66-NH2
λ
Notes: The conditions for the photooxidation of p methoxy benzyl alcohol are as follows. 10 percent molar equivalence of MOF with the substrate in acetonitrile and held under oxygen atmosphere. The source of light comes from a xenon lamp with a filter that blocks out wavelengths below 305 nm. And to reiterate the MOFs I just talked about were mil47, mil 125 and uio66.

## Slide 17: Purification of Starting Material
A
B
C D
A
B
D C
Impurities at
  3.81 ppm
  3.90 ppm
  4.46 ppm
  9.89 ppm
Notes: But first I had to purify the benzyl alcohol before I could work with it as it has all the impurities shown here.

## Slide 18: Column Purified Substrate
A
B
C D
A
B
D C
20% Ethyl acetate in hexanes to remove impurities
Ethyl acetate to recover pure product
Notes: So I ran a column with 20% ethyl acetate in hexanes followed by just ethyl acetate to obtain this pure compound.

## Slide 19: Photoreactor Setup
Notes: So before I run my model reaction I should tell you all about the photoreactor. The sample vial sits right in front of the xenon lamp with a constant flow of oxygen. There is also a fan and thermometer used to monitor the temperature and keep it at around 25 celcius.

## Slide 20: Photoreactor Setup
Notes: But in reality its just a cardboard box with a bunch of balloons sticking out of it.

## Slide 21: Photooxidation of benzyl alcohol
  24 hours
  Filter out MOF
  Rotoevaporate solvent
  1H NMR in CDCl3
Notes: So I found that I was able to actually perform photocatalysis with the mof and that NMR was a viable method for monitoring this conversion.

## Slide 22: Objectives of My Research
Develop a model for understanding the photoredox capabilities of MOFs
Task 1
  Prepare MOFs that can do photoredox catalysis
Task 2
  Set up experimental protocol for visible light photooxidation of benzyl alcohol
Task 3
  Investigate photochemical characteristics
    Kinetics
    Photochemical quantum yield
    Temperature dependence
    Mechanism
Notes: And now that I set up an experimental protocol for the visible light photooxidation of my benzyl alcohol I was able to then move onto the next task and monitor the kinetics of the reaction.

## Slide 23: Kinetics Study
M
SM
P
Notes: I monitored the reaction over the course of a 24 hour period by NMR spectroscopy. Here you can see the methoxy peak for the product at zero hours and there isn’t any. But over time we see it start to appear. The mesitylene is kept at a constant concentration to be used as an internal standard. From integration values the actual concentration for the product and starting material can be obtained as the ratio of either product or starting material to mesitylene .

## Slide 24: Calculating Concentrations
[

## Slide 25: Rate of Reaction
13% conversion
Starting material
Product
Notes: I plotted those concentration values against time to obtain this plot. As you can see the reaction is a zero order reaction and had a conversion of 13%. It is important to note how the rates for the disappearance of SM and appearance of product are about equal. This tells us that the starting material isn’t decaying into side products.

## Slide 26: Rate of Reaction
1% conversion
Starting material
Product
Notes: Interestingly, MIL47 showed essentially no catalytic activity. 1% conversion is about what we get when we do the reaction in the absence of MOF.

## Slide 27: Rate of Reaction
12% conversion
Starting material
Product
Notes: The performance of UiO 66 was similar to that of mil 125, showing a total conversion of 12% and a very similar slope.

## Slide 28: Photochemical Quantum Yield
Heterogeneous quantum yield
  Number of reactions per photon strike
  Standard Reaction
Serpone, N.; Salinaro, A. Pure and Appl. Chem. 1999, 71, 303-320.
Notes: With the rates of reactions I could then calculate photochemical quantum yield. Heterogenous photochemical quantum yield is defined as the ratio of the initial rates of the reaction to that of a standard multiplied by the quantum yield of the standard. The standard reaction was the decomposition of p-cresol and has a quantum yield of 22%

## Slide 29: Photochemical Quantum Yields
MOF | Rate (µM/Lmin) | Quantum Yield
Standard | -239.0 +/- 19.2 | 0.22 +/- 0.04
MIL-125-NH2 | -40.5 +/- 9.0 | 0.037 +/- 0.011
MIL-47-NH2 | -5.0 +/- 4.8 | 0.0046 +/- 0.0045
UiO-66-NH2 | -43.7 +/- 3.5 | 0.040 +/-0.009
Notes: This table summarizes my results. Mil 125 and uio66 had a quantum yield of about 4 percent. And youll notice that the error for mil47 is equal to it’s a value so essentially has no quantum yield.

## Slide 30: Future Work
Temperature dependence studies
Study mechanism of photooxidation
Improve MOF features for more efficient photoredox catalysis
Explore other substrates
Notes: So my research is still a work in progress. Next I would like to do temperature dependence studies and do an inhibition study to probe the mechanism. I would also like to improve the MOFs by modifying the linker and also explore other substrates.

## Slide 31: Conclusions
  MOFs were able to catalyze oxidation of benzyl alcohol
    MIL-47-NH2 shows no catalytic activity
  Reaction happens at the surface, not in the pores
    Rates are very slow
    Quantum yields are very low
Notes: In conclusion my MOFs were able to catalyze the oxidation of benzyl alcohol, with the exception of mil47. We concluded that since the rates and quantum yields are very low that the reaction happens at the surface and not in the pores.

## Slide 32: Acknowledgements
Dr. Fernando Uribe-Romo
Romo group
Family
Dr. Frank Kujawa

## Slide 33: References
Chen, T.-H.; Popov, I.; Kaveevivitchai, W.; Miljanic, O. S., Metal-Organic Frameworks: Rise of the Ligands. Chem. Mater. 2014, 26, 4322-4325.
Prier, C. K.; Rankic, D. A.; MacMillan, D. W. C., Visible Light Photoredox Catalysis with Transition Metal Complexes: Applications in Organic Synthesis. Chem. Rev. 2013, 113, 5322-5363.
Schneider, J.; Matsuoka, M.; Takeuchi, M.; Zhang, J.; Horiuchi, Y.; Anpo, M.; Bahnemann, D. W., Understanding TiO2 Photocatalysis: Mechanism and Materials. Chem. Rev. 2014, 114, 9919-9986.

## Slide 35: Inhibition Study
Scavenger Scavenges for
tBuOH •OH
DMSO •OH
Oxalate h+ in metal
K2S2O8 e- in metal
Benzoquinone superoxide
NaN3 singlet oxygen

## Slide 36: Decomposition of p-Cresol
Serpone, N.; Salinaro, A. Pure and Appl. Chem. 1999, 71, 303-320.

## Slide 37: Ru(bipyridine)3+2

## Slide 38: Optimization of MIL-47-NH2
X = NH2
Procedure | Metal : Ligand | [VCl3] | % Yield
Literature | 1 : 1 | 0.58 M | 15
Lit. + TEA | 1 : 1 | 0.58 M | 0
Experimental | 1 : 0.25 | 0.18 M | 62
Exp. + TEA | 1 : 0.25 | 0.18 M | 57
TEA
Adjusting the concentration to 0.18 M and metal to ligand ratio to 1: 0.25 increases the yield. Adding TEA enhances reproducibility.

## Slide 39: Curve Smoothing
Exponential curve smoothing
  Two peaks at 3.81 ppm merge into one
  Impurity appears absent

## Slide 40: Kinetics with pure benzyl alcohol
Standard deviations still too high
Rates for decomposition of SM and appearance of product orders of magnitude apart

## Slide 41: Summary
Crystallized several metal-organic frameworks
Showed that these MOFs possess non-trivial photooxidative capabilities
Determined the rate of reaction
Determined photochemical quantum yield

## Slide 42: Oxidation with CCl3Br
λ